Synthesis and growth mechanism of bamboo like N-doped CNT/Graphene nanostructure incorporated with hybrid metal nanoparticles for overall water splitting

Anchu Ashoka, Anand Kumara, Janarthanan Ponrajb, Said A. Mansourb

- Department of Chemical Engineering

College of Engineering, Qatar University, P O Box – 2713, Doha, Qatar

b. Qatar Environment and Energy Research Institute (QEERI)

Hamad Bin Khalifa University, Qatar Foundation, PO Box 34110, Doha, Qatar

Figure S1: EDX profile of NiCo@CNT and NiCoS@CNT. Table shows the corresponding elemental composition ( in atomic %)

Figure S1: EDX profile of NiCo@CNT and NiCoS@CNT. Table shows the corresponding elemental composition ( in atomic %)

Figure S2: BET pore size distribution curve of as-synthesized catalyst.

Figure S2: BET pore size distribution curve of as-synthesized catalyst.

Figure S3: Different types of carbon formation on the surface of NiCo@CNT.

Figure S3: Different types of carbon formation on the surface of NiCo@CNT.

Figure S4: TEM image of the formation of a) complete and b) incomplete knots in bamboo CNTs

Figure S4: TEM image of the formation of a) complete and b) incomplete knots in bamboo CNTs

Figure S5: HRTEM of bimetallic NiCo particle encapsulated with graphene layer.

Figure S5: HRTEM of bimetallic NiCo particle encapsulated with graphene layer.

Figure S6: Asymmetric elongation of NiCo catalyst during CNT formation

Figure S6: Asymmetric elongation of NiCo catalyst during CNT formation

Figure S7: TEM image of NiCoS@CNT with bamboo like carbon tubes

Figure S7: TEM image of NiCoS@CNT with bamboo like carbon tubes

Table S1: Surface elemental composition from XPS analysis.

| Element | NiCo@CNT, Atomic con (%) | NiCoS@CNT, Atomic con (%) |
| --- | --- | --- |
| Nickel (Ni) | 1.12 | 5.36 |
| Cobalt (Co) | 1.00 | 4.64 |
| Carbon (C) | 92.04 | 67.83 |
| Oxygen (O) | 2.04 | 13.60 |
| Nitrogen (N) | 3.80 | 6.92 |
| Sulphur (S) | - | 1.65 |

Figure S8: XPS C1s deconvolution profile of a)NiCo@CNT and b) NiCoS@CNT

Figure S8: XPS C1s deconvolution profile of a)NiCo@CNT and b) NiCoS@CNT

Figure S9: a)Schematic representation of N bonded graphene lattice network. N 1s XPS deconvolution spectrum of b) NiCo@CNT and c) NiCoS@CNT.

Figure S9: a)Schematic representation of N bonded graphene lattice network. N 1s XPS deconvolution spectrum of b) NiCo@CNT and c) NiCoS@CNT.

Figure S10: XPS S 2p deconvolution profile of NiCoS@CNT.

Figure S10: XPS S 2p deconvolution profile of NiCoS@CNT.

Figure S11: Magnified redox peak between 1.2 V and 1.45 V in the LSV OER profile of NiCo@CNT and NiCoS@CNT.

Figure S11: Magnified redox peak between 1.2 V and 1.45 V in the LSV OER profile of NiCo@CNT and NiCoS@CNT.

Table S2. Electrochemical parameters obtained by fitting EIS data into the equivalent circuit in Figure 8c inset

| Catalyst | Potential | Rs (Ω) | Rct (Ω) |
| --- | --- | --- | --- |
| NiCoS@CNT | 1.5 | 7.8 | 31 |
|  | 1.6 | 7.2 | 24 |
|  | 1.65 | 6.8 | 22 |
|  | 1.7 | 5.4 | 21 |
|  | 1.75 | 3.2 | 14 |
| NiCo@CNT | 1.5 | 12.7 | 46 |
|  | 1.6 | 11.4 | 44 |
|  | 1.65 | 12.1 | 38 |
|  | 1.7 | 10.6 | 36 |
|  | 1.75 | 10.9 | 31 |

Table S3. Comparison of electrochemical HER and OER performance of various Ni-Co based catalyst in alkaline medium

| Catalyst | Synthesis method | HER |  | OER |  | Overall water splitting | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | η 10 (mV vs RHE) | Tafel slope (mVdec-1) | η 10 (mV vs RHE) | Tafel slope (mVdec-1) | Cell Voltage (V) |  |
| NiCoS@CNT | Pyrolysis Melamine | 198 | 87 | 295 | 78 | 1.53 | This work |
| Ni2−xCoxP | Solid-state phosphorization | 290 | 45.2 | 270 | 65.7 | 1.65 | 1 |
| CoFePO/NF | Spray deposition | 87.5 | 118 | 274.5 | 101 | 1.91 | 2 |
| NiCoP | Plasma-assisted approach t | 32 | 87 | 280 | 37 | 1.58 | 3 |
| NiCoPS/CC | Hydrothermal | 110 | 30.4 | 230 | 63.3 | 1.54 | 4 |
| NiCo2S4 NW/NF | Direct growth | 210 | 58.9 | 260 | 40.1 | 1.63 | 5 |
| Co3FeNx (NSP-Co3FeNx) | Nitridation reaction | 23 | 94 | 222 | 46 | 1.539 | 6 |
| CFP/NiCo2O4/Co0.57Ni0.43LMO |  | 52 | 34 | 340 | 63 | 1.5 | 7 |
| NiCo2O4 | Solvothermal | 110 | 49.7 | 1.52 V | 53 | 1.65 | 8 |
| NiCo2O4 NA/CC | Topotactic conversion | 305* | 52 | 340* | 64 | 1.68 | 9 |
| NiCo2Px/CNTs | Phosphorization | 47 | 81 | 284 | 66.5 | 1.67 | 10 |

* Current Density @100 mAcm-2.

References

1. Li J, Yan M, Zhou X, et al. Mechanistic insights on ternary Ni2− xCoxP for hydrogen evolution and their hybrids with graphene as highly efficient and robust catalysts for overall water splitting. Advanced Functional Materials. 2016;26(37):6785-6796.

2. Du S, Ren Z, Zhang J, et al. Co 3 O 4 nanocrystal ink printed on carbon fiber paper as a large-area electrode for electrochemical water splitting. Chemical Communications. 2015;51(38):8066-8069.

3. Liang H, Gandi AN, Anjum DH, Wang X, Schwingenschlögl U, Alshareef HN. Plasma-assisted synthesis of NiCoP for efficient overall water splitting. Nano letters. 2016;16(12):7718-7725.

4. Li J, Xia Z, Zhou X, Qin Y, Ma Y, Qu Y. Quaternary pyrite-structured nickel/cobalt phosphosulfide nanowires on carbon cloth as efficient and robust electrodes for water electrolysis. Nano Research. 2017;10(3):814-825.

5. Sivanantham A, Ganesan P, Shanmugam S. Hierarchical NiCo2S4 nanowire arrays supported on ni foam: An efficient and durable bifunctional electrocatalyst for oxygen and hydrogen evolution reactions. Advanced Functional Materials. 2016;26(26):4661-4672.

6. Wang Y, Liu D, Liu Z, Xie C, Huo J, Wang S. Porous cobalt–iron nitride nanowires as excellent bifunctional electrocatalysts for overall water splitting. Chemical Communications. 2016;52(85):12614-12617.

7. Yin J, Zhou P, An L, et al. Self-supported nanoporous NiCo 2 O 4 nanowires with cobalt–nickel layered oxide nanosheets for overall water splitting. Nanoscale. 2016;8(3):1390-1400.

8. Gao X, Zhang H, Li Q, et al. Hierarchical NiCo2O4 hollow microcuboids as bifunctional electrocatalysts for overall Water‐Splitting. Angewandte Chemie International Edition. 2016;55(21):6290-6294.

9. Liu D, Lu Q, Luo Y, Sun X, Asiri AM. NiCo 2 S 4 nanowires array as an efficient bifunctional electrocatalyst for full water splitting with superior activity. Nanoscale. 2015;7(37):15122-15126.

10. Huang C, Ouyang T, Zou Y, Li N, Liu Z. Ultrathin NiCo 2 P x nanosheets strongly coupled with CNTs as efficient and robust electrocatalysts for overall water splitting. Journal of Materials Chemistry A. 2018;6(17):7420-7427.