Supplementary Material

Christian Randell Arro, Assem Taha Ibrahim Mohamed, Nasr Bensalah *

Department of Chemistry and Earth Sciences, College of Arts and Sciences, Qatar University,           
P.O. Box 2713, Doha, Qatar

*: Corresponding author: Phone: +97444036540; E-mail: nasr.bensalah@qu.edu.qa

Figure S.1 - SEM images of clustered Ge micro particles at three different magnifications before the addition of graphene oxide.

Figure S.2 – SEM EDX analysis performed for three composites of (a) GeO2/Ge25/r-GO, (b) GeO2/Ge25/r-GO and (c) GeO2/Ge25/r-GO. Confirming the presence of Ge, GeO2 and C components.

Figure S.3 - TGA plot of GeO2/Ge50/r-GO showing gradual decrease into a sharp decrease due to rGO decomposition.

Figure S.4 – (a) N2 Isotherm for absorption and desorption, (b) & (c) BJH Pore Volume Distribution for Adsorption and Desorption, respectively. (d) and (e) BJH Pore Area Distribution for Adsorption and Desorption, respectively.

Figure S.5.a – Post-mortem XRD plot of GeO2/Ge25/r-GO at the three stages (black) ESF, (Red) Post-Charge and (Blue) Post-Discharge.

Figure S.5.b – Post-mortem XRD plot of GeO2/Ge50/r-GO at the three stages (black) ESF, (Red) Post-Charge and (Blue) Post-Discharge.

Figure S.5.c – Post-mortem XRD plot of GeO2/Ge75/r-GO at the three stages (black) ESF, (Red) Post-Charge and (Blue) Post-Discharge.

Figure S.5.d – Post-mortem XRD of GeO2/Ge25/r-GO at ESF for peak identification of carbon, GeO2 and Ge components.

Figure S.5.e – Post-mortem XRD of GeO2/Ge50/r-GO at ESF for peak identification of carbon, GeO2 and Ge components.

Figure S.5.f – Post-mortem XRD of GeO2/Ge75/r-GO at ESF for peak identification of carbon, GeO2 and Ge components.

Figure S.5.g – Post-mortem XRD of GeO2/Ge25/r-GO at PC for peak identification.

Figure S.5.h – Post-mortem XRD of GeO2/Ge50/r-GO at PC for peak identification.

Figure S.5.I – Post-mortem XRD of GeO2/Ge75/r-GO at PC for peak identification.

Figure S.5.j – Post-mortem XRD of GeO2/Ge25/r-GO at PD for peak identification.

Figure S.5.k – Post-mortem XRD of GeO2/Ge50/r-GO at PD for peak identification.

Figure S.5.l – Post-mortem XRD of GeO2/Ge75/r-GO at PD for peak identification.

Figure S.6 – Post-mortem SEM of GeO2/Ge25/r-GO at scales of  5 um (top) & 10 um (bottom) for (a) and (d) ESF, (b) and (e) PD and (c) and (f) for PC.

Figure S.7 – Post-mortem SEM of GeO2/Ge50/r-GO at a scale of 10 um for (a) ESF, (b) PD and (c) PC.

Figure S.8 – Post-mortem SEM of GeO2/Ge75/r-GO at scale of  5 um (top) & 10 um (bottom) for (a) and (d) ESF, (b) and (e) PD and (c) and (f) for PC.

Figure S.9 – Post-mortem TEM of GeO2/Ge25/r-GO at scales of 100nm (top) & 50nm (bottom) for (a) and (d) ESF, (b) and (e) PD and (c) and (f) for PC.

Figure S.10 – Post-mortem TEM of GeO2/Ge50/r-GO at mixed scales of 100-200nm for (a) ESF, (b) PD and (c) PC.

Figure S.11 – Post-mortem TEM of GeO2/Ge75/r-GO at mixed scales of 50-100nm for (a) ESF, (b) PD and (c) PC.

Figure S.12 - Fringing subsection from post-mortem  HRTEM at a scale of 5 nm for the GeO2/Ge75/r-GO composite structure after PD as identification for the (310) Ge4Li15 plane.

5 nm

Figure S.13 - Fringing subsection from post-mortem HRTEM at a scale of 5 nm for the GeO2/Ge75/r-GO during ESF stage with d-spacing at approximately of 3.2 Å.

Figure S.14 - Broad-scan survey of Post-mortem samples from 0 to 1200 eV showing multiple strong signals including: Ge 3d, Ge 3p, Ge 3s, C 1s, Ge LMM, O 1s, Cu LMM, F 1s, F KLL and O KLL.

Figure S.15 - Detailed Post-mortem XPS Spectra of O 1s from 525 to 540 eV at (a) ESF, (b) PD and (c) PC.