Electronic Supplementary Information (ESI) File

# Nanostructural Synergism as Mn-N-C Channels in Manganese (IV) Oxide and Fluffy g-C3N4 Layered Composite with Exceptional Catalytic Capabilities

Ammar Bin Yousaf a*, Sifani Zavahir a, Akif Zeb b, Alena Michalcova c and Peter Kasak a*

a Center for Advanced Materials, Qatar University, Doha 2713, Qatar

b School of Physics and Telecommunication Engineering, South China Normal University, 51006 Guangzhou, Guangdong, P.R. China

c Department of Metals and Corrosion Engineering, University of Chemistry and Technology in Prague, Technicka 5, Prague 6, 166 28, Czech Republic

* Corresponding Authors E-mails: ammar@mail.ustc.edu.cn, ammar.chemist18@gmail.com (A.B. Yousaf) and peter.kasak@qu.edu.qa (P. Kasak)

Figure S1: SEM images for MnO2/g-C3N4 catalyst taken at two different magnifications (A) at 2µm and (B) at 200 nm

Figure S2: 4-nitrophenol absorption peaks before and after the addition of NaBH4

Figure S3: UV-absorption spectrum for the reduction of 4-nitrophenol into 4-aminophenol by using g-C3N4 catalyst.

Figure S4: Time-dependent degradation of MB in the photocatalysis reaction under visible light irradiation for g-C3N4 catalyst

Figure S5: Comparison of ORR activity for g-C3N4 and MnO2/g-C3N4 catalysts at 1600 rpm in O2 saturated 0.1 M KOH solution.

Figure S6: Accelerated durability test for ORR activity of MnO2/g-C3N4 catalyst at 1600 rpm in O2 saturated 0.1 M KOH with 10 mV/s scan rate up to 1000 cycles.

Table S1: Comparison of 4-NP reduction performance of MnO2/g-C3N4 (this work) catalyst with reported materials. “Time (min) = reduction time & K (min-1) calculated rate constant”.

| Sr. No. | Catalyst | Time (min) | K (min-1) | Ref. No. |
| --- | --- | --- | --- | --- |
| 1 | MnO2/g-C3N4 | 6 | 0.734 | This work |
| 2 | Au@MnO2 | 10 | 0.2898 | 1 |
| 3 | Ag/g-C3N4/CS | 25 | 0.14816 | 2 |
| 4 | Pd–Ni/rGO | 13 | 0.1596 | 3 |
| 5 | SiO2/Au/g-Fe2O3 | 13 | 0.396 | 4 |
| 6 | Fe3O4@Au | 16 | 0.0114 | 5 |
| 7 | Ag/g-C3N4 | 40 | 0.094 | 6 |

Table S2: Comparison of MB degradation performance of MnO2/g-C3N4 (this work) catalyst with reported materials. “Time (min) = degradation time & K (min-1) calculated rate constant”.

| Sr. No. | Catalyst | Time (min) | K (min-1) | Ref. No. |
| --- | --- | --- | --- | --- |
| 1 | MnO2/g-C3N4 | 22 | 0.208 | This work |
| 2 | MnO2 (nanosheets) | 60 | 0.00355 | 7 |
| 3 | β-MnO2 | 120 | - | 8 |
| 4 | PProDOT/MnO2 | 120 | 0.0931 | 9 |
| 5 | g-C3N4/TiO2 | 100 | 0.0231 | 10 |
| 6 | ZnO/g-C3N4 | 120 | 0.01993 | 11 |
| 7 | g-C3N4/Ca2Fe2O5 | 50 | 0.058 | 12 |

- X. Zhou, G. Zhao, M. Chen, W. Gao, X. Zhou, X. Xie, L. Yang, G. Du, Facile and Green Approach To Prepare Nanostructured Au@MnO2 and Its Applications for Catalysis and Fluorescence Sensing of Glutathione in Human Blood, ACS Sustain, Chem. Eng. 6,3 (2018) 3948–3956.

- J. An, Q. Yang, Q. Luo, X. Li, R. Yin, F. Liu, D. Wang, Preparation and characterization of silver/g-carbon nitride/chitosan nanocomposite with photocatalytic activity, Integrated Ferroelectrics, 180 (2017) 52-60.

- T. Revathy, S. Dhanavel, T. Sivaranjani, V. Narayanan, T. Maiyalagan, A. Stephen, Highly active graphene-supported palladium-nickel alloy nanoparticles for catalytic reduction of 4-nitrophenol, Appl. Surf. Sci. 449 (2018) 764-771.

- L. B. Ren, C. Teng, L. Zhu, J. He, Y. Wang, X. B. Zuo, M. Hong, Y. Wang, B. W. Jiang, J. Zhao, Preparation of uniform magnetic recoverable catalyst microspheres with hierarchically mesoporous structure by using porous polymer microsphere template, Nanoscale Res. Lett. 9 (2014) 163.

- F. Zou, Q. Ding, V. T. Tran, G. Wang, Y. Zhang, S. Kang, J. Lee, H. Zhou, Magnetically recyclable catalytic activity of spiky magneto-plasmonic nanoparticles, RSC Adv. 5 (2015) 56653-56657.

- B. Yu, Y. Liu, G. Jiang, D. Liu, W. Yu, H. Chen, L. Li, Q. Huang, Preparation of electrospun Ag/g-C3N4 loaded composite carbon nanofibers for catalytic applications, Mater. Res. Express 4 (2017) 015603.

- Y. He, D. Jiang, J. Chen, D. Jiang, Y. Zhang, Synthesis of MnO2 nanosheets on montmorillonite for oxidative degradation and adsorption of methylene blue, Journal of Colloid and Interface Science 510 (2018) 207–220.

- G. Cheng, L. Yu, T. Lin, R. Yang, M. Sun, B. Lan, L. Yang, F. Deng, A facile one-pot hydrothermal synthesis of β-MnO2 nanopincers and their catalytic degradation of methyleneblue, Journal of Solid State Chemistry 217 (2014) 57–63.

- R. Jamal, L. Zhang, M. Wang, Q. Zhao, T. Abdiryim, Synthesis of poly(3,4-propylenedioxythiophene)/MnO2 composites and their applications in the adsorptive removal of methyleneblue, Progress in Natural Science: Materials International 26 (2016) 32–40.

- M. H. Barzegar, M. M. Sabzehmeidani, M. Ghaedi, V. M. Avargani, Z. Moradi, V. A. L. Roy, H. Heidari, S-scheme heterojunction g-C3N4/TiO2 with enhanced photocatalytic activity for degradation of a binary mixture of cationic dyes using solar parabolic trough reactor, Chemical Engineering Research and Design 174 (2021) 307–318.

- D. R. Paul, S. Gautam, P. Panchal, S. P. Nehra, P. Choudhary, A. Sharma, ZnO-Modified g-C3N4: A Potential Photocatalyst for Environmental Application, ACS Omega 5 (2020) 3828−3838.

- D. S. Vavilapalli, R. G. Peri, R. K. Sharma, U. K. Goutam, B. Muthuraaman, M. S. R. Rao, S. Singh, g‑C3N4/Ca2Fe2O5 heterostructures for enhanced photocatalytic degradation of organic effluents under sunlight, Scientific Reports, 11 (2021)19639.