ELECTRONIC SUPPORTING INFORMATION

Magnesium recovery from Desalination Reject Brine as pretreatment for Membraneless Electrolysis

Nafis Mahmud1, Daniela V. Fraga Alvarez2, Mohamed H Ibrahim1, Muftah H El‐Naas1*, Daniel V. Esposito2

1Gas Processing Center

Qatar University

P.O. Box 2713, Al Tarfa Street

Doha, Qatar

2Department of Chemical Engineering

Columbia University in the City of New York

500 W. 120th St., New York, NY 10027

Corresponding Author

Muftah El Naas: muftah@qu.edu.qa

Daniel Esposito : de2300@columbia.edu

Table of Contents

| Section | Page |
| --- | --- |
| I. | Schematic of Pt¦Ti foil and Pt¦CF electrodes………………………..…...…………S2 |
| II. | Electrochemical Surface Area (ECSA) of Pt¦CF electrodes…………..……………S2 |
| III. | Polarization Curves before and after stability test………………………………….S3 |
| IV. | EDS maps of Pt¦CF electrodes after stability test……………………………...….. S4 |
| V. | Initial and final series resistance before and after stability test…………………….S5 |

- Schematic of Pt|Ti foil and Pt|CF electrodes

Figure S1. Schematic of a) platinum titanium foil (Pt|Ti Foil) and b) platinum carbon foam (Pt|CF) electrodes used as the anode and the cathode, respectively.

- Electrochemical Surface Area (ECSA) of Pt|CF electrodes

Figure S2. Cyclic voltammetry conducted in 0.5 M H2SO4 from -0.09 V vs. RHE to 1.2 V vs. RHE at 50 mV s-1 and 10 ml min-1 for 38 cycles. Final cycle was used to calculate the ECSA and it is shown in the figure.

Table 1: Geometric and electrochemical surface area of fabricated electrodes tested in different electrolyte solutions.

| Electrolyte solution | ECSA (cm2 Pt) | ECSA /Geometric area |
| --- | --- | --- |
| 1M NaCl | 36.3 | 18.2 |
| 1M NaCl+1.2 mM MgCl2 | 25.9 | 12.9 |
| 1M NaCl+5 mM MgCl2 | 33.7 | 16.8 |
| 1M NaCl+120 mM MgCl2 | 37.2 | 18.6 |

- Polarization curves before and after stability test

Figure S3. Polarization curves for the HER reaction at a cathodic volumetric flow rate of 5 ml min-1 in a) 1 M NaCl (0 mM [Mg2+], green) b) 1 M NaCl + 1.2 mM MgCl2 (1.2 mM [Mg2+], red), c) 1M NaCl + 5 mM MgCl2 (5 mM [Mg2+], yellow), and d) 1 M NaCl + 120 mM MgCl2 (120 mM [Mg2+], blue) electrolyte comparing the initial (solid line) and final (dash line) performance of the electrode after the 3-hour stability test.

- EDS maps of Pt|CF electrodes after stability test

Figure S4. Energy dispersive X-ray spectroscopy (EDS) of platinize carbon foam cathodes after 3-hour stability test. EDS mapping of the samples was conducted at a magnitude of 23X at 10 kV. In the figure, elements are sort by rows where orange represents carbon (C - a, b, c, and d), green represents platinum (Pt-f, g, h, and i), red represents magnesium (Mg-j, k, l), yellow represents sodium (Na-m, n, o, and p), and blue represents chloride ions (Cl- q, r, s, and t).  Each column shows the qualitative analysis of Pt|CF after being tested in 1M NaCl (a, f, m, and q), 1M NaCl+1.2 mM MgCl2 (b, g, j, n, and r), 1M NaCl+5 mM MgCl2 (c, h, k, o, and s), and 1M NaCl+120 mM MgCl2 (e, i, l, p, and t) for 3 hours applying 50 mA cm-2 at 10 ml min-1.

- Initial and final series resistance before and after stability test

Table S2: Average initial and final resistance measured by electrochemical impedance spectroscopy (EIS) between a frequency range of 200 Hz to 100 mHz , an AC amplitude of 10 mV at 0 V vs. RHE in a stagnant electrolyte. Table shows 95% confidence interval based on 5 measurements. Series resistance were measure between the Pt|CF as the working electrode, Pt|Ti foil as the counter electrode, and Ag/AgCl as the reference electrode.

| Electrolyte solution | Avg. Initial Resistance (Ω) | Avg. Final Resistance (Ω) |
| --- | --- | --- |
| 1M NaCl | 5.90 ± 0.20 | 7.29 ± 0.04 |
| 1M NaCl+1.2 mM MgCl2 | 4.13 ± 0.04 | 4.35 ± 0.14 |
| 1M NaCl+5 mM MgCl2 | 7.77 ± 0.14 | 8.70 ± 0.27 |
| 1M NaCl+120 mM MgCl2 | 6.72 ± 0.62 | 8.70 ± 0.09 |