Electrocatalytic conversion of CO2 over in-situ grown Cu microstructures on Cu and Zn foils

Anchu Ashok1, Anand Kumar1,*, Mohammed Ali Saleh Saad1,2, Mohammed J Al-Marri1

- Department of Chemical Engineering, College of Engineering, Qatar University, Doha, P O Box 2713, Qatar

- Gas Processing Center, College of Engineering, Qatar University, Doha, P O Box 2713, Qatar

* Corresponding author: akumar@qu.edu.qa; phone: (+974) 4403 4164

Calculation of Faradaic Efficiency (%)

The GC/HPLC signals of known concentrations of formic acid/acetate/methanol were determined and calibration curve was obtained as:

- Area (Y) = 5.4 x 10^6 x X(moles) + 1.5 x 10^5

Using this calibration curve, we can determine the concentration of formic acid/acetate/methanol in the electrolyte after 30-minute CA run:

- Concentration of formic acid =  [Area (Y)- 1.5 x 10^5] / 5.4 x 10^6

The total volume of catholyte in cathodic compartment is 0.013 L. Hence, the number of moles of formic acid/acetate/methanol in the electrolyte is (N):

- N= Volume x Concentration of formic acid

No: of moles of electrons required to reduce CO2 to formic acid/acetate/methanol (Output) = N x theoretical no: of electrons exchanged to form the desired products

- Input = Q/F

F = Faraday constant, 96485 C mol-1; and Q = measured charge

- Measured charge (Q) during CO2 conversion = I x t

I : measured current during chronoamperometric analysis

Faradaic efficiency (%) = Output / Input

Figure S1: Photograph of a) bare Cu foil and b) Cu particle loaded Cu foil.

Figure S1: Photograph of a) bare Cu foil and b) Cu particle loaded Cu foil.

Figure S2: EDX spectrum and the corresponding elemental composition of a) Cu/Cu foil and b) Cu/Zn foil.

Figure S2: EDX spectrum and the corresponding elemental composition of a) Cu/Cu foil and b) Cu/Zn foil.

Figure S3: O 1s and C 1s profile of Cu/Zn foil a-c) Fresh b-d) Used sample, respectively.

Figure S3: O 1s and C 1s profile of Cu/Zn foil a-c) Fresh b-d) Used sample, respectively.

Table S1: Comparison of faradaic efficiency of methanol and formic acid with recently reported work.

| Catalyst | Synthesis Method | Formic acid efficiency (%) | Methanol (%) | Potential | Medium | Ref |
| --- | --- | --- | --- | --- | --- | --- |
| Cu/Cu foil | Hydrothermal | 78 |  | -0.3 V (vs RHE) | 0.1 M KHCO3 | This work |
| Cu/Zn foil | Hydrothermal | 28 | 48 | -0.5 V HCOOH -1.0 V CH3OH (vs RHE) | 0.1 M KHCO3 | This work |
| Cu nanowire | Two step synthesis | 17 |  | -1.1 V vs. RHE | 0.1 M KHCO3 | [1] |
| Cu NPs | Direct reduction methods | 37 |  | −1.4 V | 0.1 M KHCO3 | [2] |
| Polyaniline- Pt | Electrodeposition | 1.5 | 0.1 | -0.8 V | 0.1 M KHCO3 | [3] |
| Pd/Cu2O–Cu | Simple one‐pot method | 92 |  | −0.25 V | 0.5 m NaHCO3 | [4] |
| Cu2O/C | Reduction Method | 8.4 |  | −1.9 V | 0.15 M of NaCl in methanol | [5] |
| Cu2Ag3 | Reduction method | ~ 8 | ~ 5 | -1.53 | 0.5 M KHCO3 | [6] |
| Sn/Cu foil | Electro deposition | 40 ( at 30 °C) |  |  | 0.1 M KHCO3 | [7] |
| Sn-Pb-Sb alloy | Electrochemical oxidation | 84 |  | -1.4 V | 0.1 M KHCO3 | [8] |
| Pd-MWNTs | Reduction | 34.5 |  |  | 0.5 M KHCO3 | [9] |
| Phosphate/Cu | Electrodeposition | ∼80 |  | -1.45 V | 0.1 M tetrabutylammonium tetrafluoroborate | [10] |
| Ni3Ga thin film |  |  | 13 | -1.38 V vs Ag/AgCl | 0.1 M K2SO4 | [11] |
| AuPt | Magnetron sputtering | 5 |  | -0.6 V | 0.1 M KHCO3 | [12] |
| Boron-doped diamond (BDD |  | 94.7 |  |  | 0.5 M KCl | [13] |
| CuO nanowire | Wet chemical | ~30 |  | - 0.6 V | 0.1 M KHCO3 | [14] |
| Pd70Pt30/C | Reduction | 88 |  | -0.4 V | 0.1 M K2HPO4 | [15] |
| PdSn/C | Wetting chemistry reduction | 99 |  | -0.43 | 0.5 M KHCO3 | [16] |
| Cu |  | ~ 30 |  | -0.9 V | 0.1 M KHCO3 | [17] |
| Cu-complex |  | ~22 |  | -0.85 | 0.5 M KHCO3 | [18] |
| Cu pillars | Electrodeposition method | 28.7 |  | - 0.5 | 0.1 M KHCO3 | [19] |
| PD-Zn/Ag foam | Pulse deposition | 4 | 10.5 % | -1.4 | 0.1 M KHCO3 | [20] |
| C-Py-Sn-Zn | Electrochemical method |  | 59.9 % | -0.5 | 0.1 M KHCO3 | [21] |
| Cu2O/ZnO | Air brushing |  | 17.7 % | -1.3 V vs Ag/AgCl | 0.5 M KHCO3 | [22] |
| Cu nanocluster-ZnO | Deposition | 7.7 | 2.8 % | -1.4 V vs Ag/AgCl | 0.1 M KHCO3 | [23] |

References

[1]	M. Ma, K. Djanashvili, W.A. Smith, Controllable Hydrocarbon Formation from the Electrochemical Reduction of CO2 over Cu Nanowire Arrays, Angew. Chemie - Int. Ed. (2016). https://doi.org/10.1002/anie.201601282.

[2]	Y.X. Duan, F.L. Meng, K.H. Liu, S.S. Yi, S.J. Li, J.M. Yan, Q. Jiang, Amorphizing of Cu Nanoparticles toward Highly Efficient and Robust Electrocatalyst for CO2 Reduction to Liquid Fuels with High Faradaic Efficiencies, Adv. Mater. (2018). https://doi.org/10.1002/adma.201706194.

[3]	D.N. Abram, K.P. Kuhl, E.R. Cave, T.F. Jaramillo, Platinum and hybrid polyaniline-platinum surfaces for the electrocatalytic reduction of CO2, MRS Commun. (2015). https://doi.org/10.1557/mrc.2015.30.

[4]	J. Li, S.X. Guo, F. Li, F. Li, X. Zhang, J. Ma, D.R. MacFarlane, A.M. Bond, J. Zhang, Electrohydrogenation of Carbon Dioxide using a Ternary Pd/Cu2O–Cu Catalyst, ChemSusChem. (2019). https://doi.org/10.1002/cssc.201901636.

[5]	N. Uemoto, M. Furukawa, I. Tateishi, H. Katsumata, S. Kaneco, Electrochemical carbon dioxide reduction in methanol at Cu and Cu2 O-deposited carbon black electrodes, ChemEngineering. (2019). https://doi.org/10.3390/chemengineering3010015.

[6]	Y. Wang, D. Wang, C.J. Dares, S.L. Marquard, M. V. Sheridan, T.J. Meyer, CO2 reduction to acetate in mixtures of ultrasmall (Cu)n,(Ag)m bimetallic nanoparticles, Proc. Natl. Acad. Sci. U. S. A. (2017). https://doi.org/10.1073/pnas.1713962115.

[7]	B. Qin, H. Wang, F. Peng, H. Yu, Y. Cao, Effect of the surface roughness of copper substrate on three-dimensional tin electrode for electrochemical reduction of CO2 into HCOOH, J. CO2 Util. (2017). https://doi.org/10.1016/j.jcou.2017.07.012.

[8]	S. Rasul, A. Pugnant, H. Xiang, J.M. Fontmorin, E.H. Yu, Low cost and efficient alloy electrocatalysts for CO2 reduction to formate, J. CO2 Util. (2019). https://doi.org/10.1016/j.jcou.2019.03.016.

[9]	G. Lu, H. Wang, Z. Bian, X. Liu, Electrochemical reduction of COto organic acids by a Pd-MWNTs gas-diffusion electrode in aqueous medium, Sci. World J. (2013). https://doi.org/10.1155/2013/424617.

[10]	Y. Zhou, Y. Xiao, J. Zhao, A local proton source from carboxylic acid functionalized metal porphyrins for enhanced electrocatalytic CO2reduction, New J. Chem. (2020). https://doi.org/10.1039/d0nj02900a.

[11]	A.R. Paris, A.T. Chu, C. B. O’Brien, J.J. Frick, S.A. Francis, A.B. Bocarsly,  Tuning the Products of CO 2 Electroreduction on a Ni 3 Ga Catalyst Using Carbon Solid Supports , J. Electrochem. Soc. (2018). https://doi.org/10.1149/2.0791807jes.

[12]	M. Ma, H.A. Hansen, M. Valenti, Z. Wang, A. Cao, M. Dong, W.A. Smith, Electrochemical reduction of CO2 on compositionally variant Au-Pt bimetallic thin films, Nano Energy. (2017). https://doi.org/10.1016/j.nanoen.2017.09.043.

[13]	K. Natsui, H. Iwakawa, N. Ikemiya, K. Nakata, Y. Einaga, Stable and Highly Efficient Electrochemical Production of Formic Acid from Carbon Dioxide Using Diamond Electrodes, Angew. Chemie - Int. Ed. (2018). https://doi.org/10.1002/anie.201712271.

[14]	M. Ma, K. Djanashvili, W.A. Smith, Selective electrochemical reduction of CO2 to CO on CuO-derived Cu nanowires, Phys. Chem. Chem. Phys. (2015). https://doi.org/10.1039/c5cp03559g.

[15]	R. Kortlever, I. Peters, S. Koper, M.T.M. Koper, Electrochemical CO2 Reduction to Formic Acid at Low Overpotential and with High Faradaic Efficiency on Carbon-Supported Bimetallic Pd-Pt Nanoparticles, ACS Catal. (2015). https://doi.org/10.1021/acscatal.5b00602.

[16]	X. Bai, W. Chen, C. Zhao, S. Li, Y. Song, R. Ge, W. Wei, Y. Sun, Exclusive Formation of Formic Acid from CO2 Electroreduction by a Tunable Pd-Sn Alloy, Angew. Chemie - Int. Ed. (2017). https://doi.org/10.1002/anie.201707098.

[17]	A. Thevenon, A. Rosas-Hernández, J.C. Peters, T. Agapie, In-Situ Nanostructuring and Stabilization of Polycrystalline Copper by an Organic Salt Additive Promotes Electrocatalytic CO2 Reduction to Ethylene, Angew. Chemie - Int. Ed. (2019). https://doi.org/10.1002/anie.201907935.

[18]	Z. Weng, Y. Wu, M. Wang, J. Jiang, K. Yang, S. Huo, X.F. Wang, Q. Ma, G.W. Brudvig, V.S. Batista, Y. Liang, Z. Feng, H. Wang, Active sites of copper-complex catalytic materials for electrochemical carbon dioxide reduction, Nat. Commun. (2018). https://doi.org/10.1038/s41467-018-02819-7.

[19]	J. Chung, D.H. Won, J. Koh, E.H. Kim, S.I. Woo, Hierarchical Cu pillar electrodes for electrochemical CO2 reduction to formic acid with low overpotential, Phys. Chem. Chem. Phys. (2016). https://doi.org/10.1039/c5cp07964k.

[20]	Q.H. Low, N.W.X. Loo, F. Calle-Vallejo, B.S. Yeo, Enhanced Electroreduction of Carbon Dioxide to Methanol Using Zinc Dendrites Pulse-Deposited on Silver Foam, Angew. Chemie - Int. Ed. (2019). https://doi.org/10.1002/anie.201810991.

[21]	W. Huang, G. Yuan, A composite heterogeneous catalyst C-Py-Sn-Zn for selective electrochemical reduction of CO2 to methanol, Electrochem. Commun. (2020). https://doi.org/10.1016/j.elecom.2020.106789.

[22]	J. Albo, A. Sáez, J. Solla-Gullón, V. Montiel, A. Irabien, Production of methanol from CO2 electroreduction at Cu2O and Cu2O/ZnO-based electrodes in aqueous solution, Appl. Catal. B Environ. (2015). https://doi.org/10.1016/j.apcatb.2015.04.055.

[23]	E. Andrews, M. Ren, F. Wang, Z. Zhang, P. Sprunger, R. Kurtz, J. Flake,  Electrochemical Reduction of CO 2 at Cu Nanocluster / (101̅0) ZnO Electrodes , J. Electrochem. Soc. (2013). https://doi.org/10.1149/2.105311jes.