Supporting Information

Nicotinamide-Based Supergelator Self-Assembling via Asymmetric Hydrogen Bonding NH…OC and H…Br- Pattern for Reusable, Shape-Persistent and Self-Healable Nontoxic Fuel Gels

Peter Kasák*,a, Peter Hrobárik*,b,c, Josef Osičkad, Dominika Solárikováe, Branislav Horváthf, Ján Tkáčg, Kishor K. Sadasivunia, Mariam A. AlMaadeed a, Roman Mikláš*,e

a Center for Advanced Materials, Qatar University, PObox 2713, Doha, Qatar

b Laboratory for Advanced Materials (LAM), Comenius University Science Park, Ilkovičova 8, SK-84215 Bratislava, Slovakia

c Department of Inorganic Chemistry, Faculty of Natural Sciences, Comenius University, Ilkovičova 6, SK-84215 Bratislava, Slovakia

d Centre of Polymer Systems, University Institute, Tomas Bata University in Zlin, Trida T. Bati 5678, CZ-76001 Zlin, Czech Republic

e Department of Chemical Theory of Drugs, Faculty of Pharmacy, Comenius University, Kalinčiakova 8, SK-83104 Bratislava, Slovakia

f Laboratory of Nuclear Magnetic Resonance, Faculty of Pharmacy, Comenius University in Bratislava, Odbojárov 10, SK-83232 Bratislava, Slovakia

g Institute of Chemistry, Slovak Academy of Sciences, Dúbravská cesta 9, SK-84538 Bratislava, Slovakia

* Corresponding authors peter.kasak@qu.edu.qa; Tel: +974 4403 5674. peter.hrobarik@uniba.sk; miklas@fpharm.uniba.sk.

- Experimental section

Synthesis and characterization of nicotinamide gelators

Scheme S1. Synthesis of nicotinamide-based gelator 1

1 g (3.08 mmol) of N,N’-[(1R,2R)-cyclohexane-1,2-diyl]dinicotin-amide (4) was mixed in autoclave with 2.35 g of 1-bromohexadecane (7.7 mmol, 2.5 eq) and 15 ml of acetonitrile. Reaction mixture was heated at 150 °C for 48 h and then allowed to cool to room temperature. The resulting solid material was suspended in a mixture of diethylether : hexane (1:1, v/v, 100 ml) and filtered off to give light brown powder. The white crystalline gelators were obtained after three crystallizations from anhydrous acetone/methanol mixture. Racemic derivative rac-1 was synthetized using the same method from racemic trans-cyclohexane-1,2-diamine.

Gelator 1: White crystals, yield = 69 %. M.p. = 175-176 °C.

1H NMR (CDCl3) δ 9.84 (s, 2H), 9.27 (d, J = 5.9 Hz, 2H), 9.04 (d, J = 8.1 Hz, 2H), 8.96 (d, J = 5.9 Hz, 2H), 8.14 (dd, J = 7.6 Hz, 7.6 Hz, 2H), 4.91 (t, J = 7.26 Hz, 4H, N+-CH2), 4.11 (s, 2H), 1.81-2.18 (m, 10H), 1.25-1.35 (m, 54H), 0.87 (t, J = 7.0 Hz, 6H, 2 × CH3).

13C NMR (CDCl3) δ 161.0, 146.0, 144.4, 144.3, 134.3, 128.3, 62.6, 54.5, 31.9, 31.7, 31.2, 29.7 (2C), 29.6 (2C), 29.5, 29.4, 29.3, 29.1, 26.2, 24.7, 22.7, 14.1.

HRMS: Calculated for C50H86N4O22+ , m/z = 387.3350, found 387.3383.

Figure S1. 1H NMR of 1 in CDCl3

Figure S2. 13C NMR of 1 in CDCl3

Figure S3. 1H-1H COSY NMR of 1 in CDCl3

Figure S4. 1H-13C HMBC NMR of 1 in CDCl3

Figure S5. 1H-13C HSQC NMR of 1 in CDCl3

Figure S6. 1H NMR of 1 in H2O/D2O (90 °C)

Figure S7. 1H-1H COSY NMR of 1 in H2O/D2O (80 °C)

Figure S8. 1H-13C HSQC NMR of 1 in H2O/D2O (80 °C)

Figure S9. HRSM of 1.

Synthesis of compound 2

Scheme S2. Synthesis of nicotinamide-based derivative 2

To 0.306 g (0.33 mmol) of 1 was added 20 ml of distilled water and the suspension was heated to 95 °C with stirring until homogenous solution was observed. To this hot solution was added dropwise a solution of KPF6 (0.181 g, 0.984 mmol) in 10 ml of distilled water and heating was turned off. Reaction mixture was allowed to slowly cool down to room temperature and mixed another 1 hour. After evaporation of water from the reaction mixture, 30 ml of DCM was added to the white residue. Suspension was stirred for 10 min and filtered. The solid residue was treated with another 30 ml of DCM for 10 min and combined DCM extracts were evaporated to dryness to afford 0.315 g (90%) of product 2 as a white powder.

M.p. = 107-108 °C.

1H NMR (CD2Cl2) δ 9.36 (s, 2H), 8.85 (d, J = 8.4 Hz, 2H), 8.55 (d, J = 6.3 Hz, 2H), 8.09 (d, J = 5.9 Hz, 2H), 8.02 (t, J = 6.3 Hz, 2H), 4.57 (t, J = 7.7 Hz, 4H, N+-CH2,), 4.07 (s, 2H), 1.59-2.09 (m, 10H), 1.20-1.47 (m, 54H), 0.88 (t, J = 6.3 Hz, 6H, 2 × CH3).

13C NMR (CD2Cl2) δ 161.2, 144.6, 144.0, 143.8, 134.8, 128.3, 62.9, 62.3, 54.9, 31.9, 31.2, 31.1, 29.7 (2C), 29.5, 29.3, 28.9, 26.1, 24.6, 22.6, 13.8.

31P NMR (CD2Cl2, 121.5 MHz) δ: -145.0, heptet (J = 713.4 Hz)

19F NMR (CD2Cl2, 282.3 MHz) δ: -182.3, doublet (J = 713.4 Hz)

HRMS: Calculated for C50H86N4O22+ , m/z = 387.3350, found 387.3407.

Figure S10. 1H NMR of 2 in CD2Cl2

Figure S11. 13C NMR of 2 in CD2Cl2

Figure S12. 31P NMR of 2 in CD2Cl2

Figure S13. 19F NMR of 2 in CD2Cl2

Figure S14. HRMS of 2.

Synthesis of compound 3

Scheme S3. Synthesis of isonicotinamide-based derivative 3

Synthesis of 3 was performed in an analogy with the procedure described for 1 (see above), but using isonicotinoyl chloride hydrochloride instead of nicotinoyl chloride hydrochloride.

3 was isolated as a white powder in 78% yield. M.p.: 277-281°C.

1H NMR (CDCl3) δ 9.29 (d, 4H, J = 6.3 Hz, Py), 9.10 (d, 2H, J = 5.9 Hz, NH), 8.69 (d, 4H, J = 6.3 Hz, Py), 4.84−4.98 (m, 4H), 4.26 (bs, 2H), 1.84-2.18 (m, 12H), 1.24-1.34 (m, 52H), 0.87 (t, 6H, J = 6.6 Hz, 2 × CH3).

13C NMR (CDCl3) δ 161.9, 148.5, 145.5, 126.9, 62.3, 54.8, 31.9, 31.8, 31.2, 29.7, 29.6, 29.5, 29.4, 29.3, 29.1, 26.2, 24.7, 22.7, 14.1.

HRMS: Calculated for C50H86N4O22+ , m/z = 387.3350, found 387.3405.

Figure S15. 1H NMR of 3 in CDCl3

Figure S16. 13C NMR of 3 in CDCl3

Figure S17. HRMS of 3.

Figure S18: Image of gels from 0.05 % w/v of 1 in glycerol (left)

and 0.035 % w/v of 1 in water (right)

Table S1. Gelation properties of compound 1 (with minimal gelation concentration in parentheses) and rac-1.

| Solvent | 1 | rac-1 |
| --- | --- | --- |
| Methanol | S | S |
| Ethanol | G (1%) | P |
| Isopropanol | G (0.1%) | G (1%) |
| Butan-1-ol | OG (2.5%) | OG |
| Octanol | G (0.1%) | G |
| 1-Decanol | OG (2.5%) | OG |
| Ethan-1,2-diol | OG (2.5%) | OG |
| Water | G (0.035%) | G (0.5%) |
| Acetone | I | I |
| Acetonitrile | I | I |
| Benzene | G (0.2%) | G (1%) |
| Toluene | G (0.2%) | G (1%) |
| p-Xylene | G (2.5%) | G (5%) |
| Chloroform | S | S |
| Ethyl acetate | I | I |
| DMSO | OG (2.5%) | S |
| Diethyl Ether | I | I |
| THF | G (1.0%) | G (2.5%) |
| Hexadecane | I | I |
| Cyclohexane | I | I |
| DMF | G (1%) | G (2%) |
| Glycerol | G (0.05%) | G (0.5%) |
| Pyridine | G (1%) | OG (2%) |

G – gel			OG – opaque gel		S – homogenous solution

I – insoluble	P – precipitation

Figure S19: Dependence of storage (G’) and loss (G’’) modulus on gelator concentration in iPrOH

Figure S20: Dependence of concentration of 1 (red cycles) and rac-1 (black squares) in water to critical gelation temperature.

Schröder-van Laar analysis

lnc=-∆HR1Tgel+const.

Figure S21. Dependence of ln (c) on 1/Tgel for 1 (red cycles) and rac-1 (black squares) in water with corresponding linear fits

Figure S22. ATR-FTIR spectrum of 2

Figure S23. ATR-FTIR spectrum of 3

Time dependent CD and UV spectra

25°C

25°C

25°C

25°C

25°C

25°C

25°C

25°C

110 °C

110 °C

110 °C

110 °C

110 °C

110 °C

Figure S24. Time dependent CD spectra of 0.2%wt 1 in iPrOH recorded at different temperature

25°C

25°C

80 °C

80 °C

80 °C

80 °C

80 °C

80 °C

25°C

25°C

25°C

25°C

Figure S25. Time dependent UV-Vis spectra of 0.2% 1 in iPrOH recorded at differ5nt temperature

25 °C

25 °C

110°C

110°C

110 °C

110 °C

25°C

25°C

Figure S26. Time dependant CD spectra of 0.2% 1 in toluene recorded at different temperature

110°C

110°C

25 °C

25 °C

Figure S27. Time dependant UV-Vis spectra of 0.2 % 1 in toluene recorded at different temperature after sample preparation

25°C

25°C

25°C

25°C

100°C

100°C

25°C

25°C

100°C

100°C

Figure S28. Time dependent CD spectra of 0.1% 1 in water recorded at at different temperature after sample preparation

100°C

100°C

25°C

25°C

Figure S29. Time dependent UV-vis spectra of 0.1% 1 in water recorded at different temperature after sample preparation

25°C

25°C

80°C

80°C

80°C

80°C

80°C

80°C

25°C

25°C

25°C

25°C

Figure S30. Time dependent CD spectra of 0.2% 2 in iPrOH recorded

at different temperature after sample preparation

80°C

80°C

25°C

25°C

Figure S31. Time dependent UV-vis spectra of 0.2% 2 in iPrOH recorded

at different temperature after sample preparation

240 mins

240 mins

120 mins

120 mins

60 mins

60 mins

0 mins

0 mins

Figure S32. Images showing moldable, colorable (cryslat violet) and shape-persistent isopropanol 1 gel (0.5 wt%) fabricated for 1 hour from six hydrogel cylinder blocks put together with and without dopped dye (cryslat violet) with indicated time after fabrication by rest in Petri dish. All tests were performed at 25 °C.

- Computational Details

Investigated monomeric structures and their self-assemblies were fully optimized at the PBE level of theory,S including an atom-pairwise correction for dispersion forces via Grimme’s D3 model with Becke−Johnson (BJ) damping S, S in the Turbomole program.S All atoms were treated with an all-electron def2-TZVPP basis set, in conjunction with an approximation of the Coulomb term by density fitting with a def2-TZVPP auxiliary basis set.S Bulk solvent effects were simulated by the conductor-like screening model (COSMO), considering isopropanol as the solvent.S The optimized structures were characterized as true minima on the potential energy hypersurface by harmonic vibrational frequency analysis performed at the same level (RI-PBE-D3(BJ)/def2-TZVPP).

The NMR shielding tensors were computed in the Gaussian 16 program packageS at the CAM-B3LYP/6-311++G** levelS by using gauge-including atomic orbitals orbitals (GIAO).S The calculated 1H and 13C NMR shieldings were converted to chemical shifts ( in ppm) relative to the shieldings of tetramethylsilane (TMS). The calculated NMR shifts were averaged over chemically equivalent nuclei.

Time-dependent DFT calculations of excitation energies were performed at the CAM-B3LYP/6-311++G** level in the Gaussian program.S7 To facilitate the comparison of theory with experiment, the calculated absorption characteristics (for first 100 excited states) were convolved with a Gaussian function having a full width at half-maximum (FWHM) of 0.2 eV with the help of the program SpecDis.S

Non-covalent interaction (NCI) regionsS were calculated with the NCI Plot programS from PBE0/6-311++G** electron densities and visualized with VMD program.S NCI Plot code enables identification of non-covalent interactions from the reduced density gradient (RDG).S11

Natural bond orbital (NBO) analyses were carried out using the NBO6 code,S interfaced with Gaussian 16.S7

Figure S33. Structures and relative energies of the local minima found for 1 dimers.

Pendant alkyl groups replaced by methyls for sake of clarity.

Relative energies of analogous N-hexadecyl derivatives are given in parenthesis.

Figure S34. Structures and relative energies of the local minima found for 1 oligomers with a hybrid NH…CO, H…Br bonding pattern (left) and with two parallel NH…CO strands (right).

Pendant alkyl groups replaced by methyls for sake of clarity.

Figure S35. Structures and relative energies of the local minima found for 1 trimers with a

hybrid (asymmetric) NH…CO, H…Br bonding pattern (bottom) and with two parallel NH…CO strands (top).

Figure S36. Structure of 2 trimer with two parallel NH…CO strands.

Figure S37. Structures and relative energies of the local minima found for 3 tetramers with a

hybrid NH…CO, H…Br bonding pattern (left) and with two parallel NH…CO strands (right).

Figure S38. NCI analysis of the 1 dimer with a hybrid NH…CO, H…Br bonding pattern

(RDG isosurfaces ± 0.4 a.u.). Alkyl groups replaced by methyl for sake of clarity.

Figure S39. Selected NCI interactions (RDG isosurfaces ± 0.8 a.u.) in 1 dimer with a hybrid NH…CO, H…Br bonding pattern: A) NH…CO interaction, B) Interaction of Br- with acidic NHamide and CHpyridine hydrogens, C) Intramolecular CO…HCpyridine interaction, D) Intermolecular CO…HetAr interaction.

Figure S40. Simulated UV-vis (top) and CD (bottom) spectra for 12+.

TD-DFT results at the CAM-B3LYP/6-311++G**/PCM level

Figure S41. Simulated UV-vis (top) and CD (bottom) spectra for trimeric 1 with two parallel NH…CO strands  (cf. Figure S35 for the structure).

TD-DFT results at the CAM-B3LYP/6-311++G**/PCM level.

Figure S42. Simulated UV-vis (top) and CD (bottom) spectra for trimeric 1 with an asymmetric NH…CO, H…Br bonding pattern (see Figure S35 for the structure).

TD-DFT results at the CAM-B3LYP/6-311++G**/PCM level.

Figure S43. Frontier MOs in trimeric 1 contributing dominantly to the first excited state (max = 330 nm). DFT results at the CAM-B3LYP/6-311++G**/PCM level.

Figure S44. Calculated 1H NMR aromatic and amidic shifts in 12+ and central unit of trimeric 1 with a hybrid NH…CO, H…Br bonding pattern (see Figure S35, bottom for the structure).

DFT results at the CAM-B3LYP/6-311++G**/PCM level.

- References

S Perdew, J. P.; Burke, K.; Ernzerhof, M. Phys. Rev. Lett. 1996, 77, 3865−3868.

S Grimme, S.; Antony, J.; Ehrlich, S.; Krieg, H. J. Chem. Phys. 2010, 132, 154104.

S Grimme, S.; Ehrlich, S.; Goerigk, L. J. Comput. Chem. 2011, 32, 1456−1465.

S TURBOMOLE, version 7.5; TURBOMOLE GmBH, a development of the University of Karlsruhe and Forschungszentrum Karlsruhe, 2020; available from: http://www.turbomole.com.

S Weigend, F.; Ahlrichs, R. Phys. Chem. Chem. Phys. 2005, 7, 3297−3305.

S Klamt, A.; Schuurmann, G. J. Chem. Soc., Perkin Trans. 2 1993, 2, 799−805.

S Gaussian 16, Revision C.01, Frisch, M. J.; Trucks, G. W.; Schlegel, H. B.; Scuseria, G. E.; Robb, M. A.; Cheeseman, J. R.; Scalmani, G.; Barone, V.; Petersson, G. A.; Nakatsuji, H.; Li, X.; Caricato, M.; Marenich, A. V.; Bloino, J.; Janesko, B. G.; Gomperts, R.; Mennucci, B.; Hratchian, H. P.; Ortiz, J. V.; Izmaylov, A. F.; Sonnenberg, J. L.; Williams-Young, D.; Ding, F.; Lipparini, F.; Egidi, F.; Goings, J.; Peng, B.; Petrone, A.; Henderson, T.; Ranasinghe, D.; Zakrzewski, V. G.; Gao, J.; Rega, N.; Zheng, G.; Liang, W.; Hada, M.; Ehara, M.; Toyota, K.; Fukuda, R.; Hasegawa, J.; Ishida, M.; Nakajima, T.; Honda, Y.; Kitao, O.; Nakai, H.; Vreven, T.; Throssell, K.; Montgomery, J. A., Jr.; Peralta, J. E.; Ogliaro, F.; Bearpark, M. J.; Heyd, J. J.; Brothers, E. N.; Kudin, K. N.; Staroverov, V. N.; Keith, T. A.; Kobayashi, R.; Normand, J.; Raghavachari, K.; Rendell, A. P.; Burant, J. C.; Iyengar, S. S.; Tomasi, J.; Cossi, M.; Millam, J. M.; Klene, M.; Adamo, C.; Cammi, R.; Ochterski, J. W.; Martin, R. L.; Morokuma, K.; Farkas, O.; Foresman, J. B.; Fox, D. J. Gaussian, Inc., Wallingford CT, 2016.

S Yanai, T.; Tew, D. P.; Handy, N. C. Chem. Phys. Lett. 2004, 393, 51–57.

S Hansen, A. E.; Bouman, T. D. J. Chem. Phys. 1985, 82, 5035−5047.

S Bruhn, T.; Schaumlöffel, A.; Hemberger, Y.; Pescitelli, G. SpecDis, version 1.71; Berlin, Germany, 2017; available from: https://specdis-software.jimdo.com.

S a) Johnson, E. R.; Keinan, S.; Mori-Sánchez, P.; Contreras-García, J.; Cohen, A. J.; Yang, W. J. Am. Chem. Soc. 2010, 132, 6498−6506; b) Contreras-García, J.; Johnson, E. R.; Keinan, S.; Chaudret, R.; Piquemal, J.-P.; Beratan, D. N.; Yang, W. J. Chem. Theory Comput. 2011, 7, 625−632.

S Boto, R. A.; Peccati, F.; Laplaza, R.; Quan, C.; Carbone, A.; Piquemal, J.-P.; Maday, Y.; Contreras-Garcia, J. NCIPLOT4: A new step towards a fast quantification of noncovalent interactions; NCI program is available from: https://github.com/juliacontrerasgarcia/nciplot.

S Humphrey, W.; Dalke, A.; Schulten, K. J. Mol. Graphics 1996, 14, 33; VMD program is available from: https://www.ks.uiuc.edu/Research/vmd.

S Glendening, E. D.; Badenhoop, J. K.; Reed, A. E.; Carpenter, J. E.; Bohmann, J. A.; Morales, C. M.; Landis, C. R.; Weinhold, F. NBO 6.0; Theoretical Chemistry Institute, University of Wisconsin: Madison, WI, 2013; available from http://nbo6.chem.wisc.edu.