Optimum sintering method and temperature for cold compact Bismuth Telluride pellets for thermoelectric applications

Farheen F. Jaldurgam1,2, Zubair Ahmad2,3*, Farid Touati1, Abdul Shakoor3, Abdulla Al Ashraf3, Dong Suk Han3, and Talal Altahtamouni4

1 Department of Electrical Engineering, College of Engineering, Qatar University, P.O. Box 2713 Doha, Qatar.

2Qatar University Young Scientist Center (YSC), Qatar University, 2713, Doha, Qatar

3Center for Advanced Materials (CAM), Qatar University, 2713, Doha, Qatar

4 Materials Science & Technology Program, College of Arts and Sciences, Qatar University, 2713, Doha, Qatar

Supplementary Data:

## Structural and phase characterization

Figure S1. XRD profile of (a) commercial p-type and n-type powders, (b) Conventional sintered p-type Bi2Te3, (c) Conventional sintered n-type Bi2Te3, (d) Tube sintered p-type Bi2Te3, (e) Tube sintered n-type Bi2Te3.

(a)

(b)

(c)

(e)

(d)

## Grain Size Calculation

Table S1. Grain Size Calculation of the various bismuth telluride samples.

| Box Furnace |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P-Type |  |  |  |  |  |  |  | N-Type |  |  |  |  |  |  |  |
| Temp | 2θ | θ | 2θ (rad) | θ (rad) | β | L | D (nm) | Temp | 2θ | θ | 2θ (rad) | θ (rad) | β | L | D (nm) |  |
| 250 | 44.55 | 22.28 | 0.78 | 0.39 | 0.16 | 13.74 | 611.47 | 250 | 17.57 | 8.79 | 0.31 | 0.15 | 0.13 | 39.78 | 698.34 |  |
| 300 | 17.48 | 8.74 | 0.31 | 0.15 | 0.09 | 57.14 | 997.84 | 300 | 17.56 | 8.78 | 0.31 | 0.15 | 0.13 | 39.80 | 698.33 |  |
| 350 | 27.56 | 13.78 | 0.48 | 0.24 | 0.06 | 51.58 | 1420.0 | 350 | 27.68 | 13.84 | 0.48 | 0.24 | 0.17 | 19.77 | 546.65 |  |
| 400 | 30.79 | 15.39 | 0.54 | 0.27 | 0.14 | 21.16 | 650.70 | 400 | 27.67 | 13.84 | 0.48 | 0.24 | 0.18 | 18.36 | 507.58 |  |
| Microwave Furnace |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| P-Type |  |  |  |  |  |  |  | N-Type |  |  |  |  |  |  |  |
| Temp | 2θ | θ | 2θ (rad) | θ (rad) | β | L | D (nm) | Temp | 2θ | θ | 2θ (rad) | θ (rad) | β | L | D (nm) |  |
| 250 | 17.48 | 8.74 | 0.31 | 0.15 | 0.12 | 44.42 | 775.91 | 250 | 17.56 | 8.78 | 0.31 | 0.15 | 0.14 | 36.19 | 634.80 |  |
| 300 | 17.55 | 8.77 | 0.31 | 0.15 | 0.13 | 39.83 | 698.32 | 300 | 17.55 | 8.77 | 0.31 | 0.15 | 0.13 | 39.83 | 698.32 |  |
| 350 | 44.57 | 22.28 | 0.78 | 0.39 | 0.14 | 15.26 | 679.44 | 350 | 27.70 | 13.85 | 0.48 | 0.24 | 0.17 | 19.75 | 546.68 |  |
| 400 | 27.58 | 13.79 | 0.48 | 0.24 | 0.08 | 42.95 | 1183.4 | 400 | 27.70 | 13.85 | 0.48 | 0.24 | 0.15 | 21.40 | 592.26 |  |
| Tube Furnace |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| P-Type |  |  |  |  |  |  |  | N-Type |  |  |  |  |  |  |  |
| Temp | 2θ | θ | 2θ (rad) | θ (rad) | β | L | D (nm) | Temp | 2θ | θ | 2θ (rad) | θ (rad) | β | L | D (nm) |  |
| 250 | 17.47 | 8.74 | 0.30 | 0.15 | 0.10 | 50.01 | 872.98 | 250 | 17.57 | 8.78 | 0.31 | 0.15 | 0.14 | 36.17 | 634.81 |  |
| 300 | 17.49 | 8.75 | 0.31 | 0.15 | 0.12 | 44.40 | 775.92 | 300 | 17.56 | 8.78 | 0.31 | 0.15 | 0.14 | 36.19 | 634.80 |  |
| 350 | 27.73 | 13.86 | 0.48 | 0.24 | 0.12 | 28.51 | 789.91 | 350 | 27.68 | 13.84 | 0.48 | 0.24 | 0.19 | 17.13 | 473.73 |  |
| 400 | 27.71 | 13.85 | 0.48 | 0.24 | 0.14 | 23.34 | 646.16 | 400 | 27.65 | 13.83 | 0.48 | 0.24 | 0.17 | 19.78 | 546.63 |  |

## SEM cross-section images

Figure S2. Field emission scanning electron microscopy (FESEM) images at 1µm of (a) pristine p-type Bi2Te3 sample, (b) BP250, (c) BP300, (d) BP350.

(d)

(c)

(b)

(a)

Figure S3. Field emission scanning electron microscopy (FESEM) images at 1µm of (a) pristine p-type Bi2Te3 sample, (b) TP250, (c) TP300, (d) TP350. Nanoparticles of sizes less than 1 µm can be observed in the SEM images of samples sintered at 300oC and 350oC.

(b)

(d)

(c)

(a)

(a)

Figure S4. Field emission scanning electron microscopy (FESEM) images at 1µm of (a) pristine p-type Bi2Te3 sample, (b) BN250, (c) BN300, (d) BN350.

(b)

(d)

(c)

Figure S5. Field emission scanning electron microscopy (FESEM) images at 1µm of (a) pristine p-type Bi2Te3 sample, (b) TN250, (c) TN300, (d) TN350. Nanoparticles of sizes less than 1 µm can be observed in the SEM images of samples sintered at 300oC and 350oC.

(a)

(b)

(d)

(c)

Figure S6. Field emission scanning electron microscopy (FESEM) images at 3µm of (a) cross-section pristine p-type Bi2Te3 sample, (b) BP300 (c) MP300, (d) TP300.

Figure S7. Field emission scanning electron microscopy (FESEM) images at 3µm of (a) cross-section pristine n-type Bi2Te3 sample, (b) BN300 (c) MN300, (d) TN300.

## DC Electrical Conductivity

Figure S8. The bar graph representing the variation of the DC electrical conductivity of bismuth telluride.

## Thermal Conductivity

Figure S9. The bar graph representing the variation of the thermal conductivity of bismuth telluride at different sintering temperatures.

## Broadband Dielectric Spectroscopy

Figure S10. The variation of the AC electrical conductivity with temperature at different frequencies of bismuth telluride sintered in box, microwave, and tube furnace at 300oC and 350oC.

Figure S11. The variation of the AC electrical conductivity with frequency at different temperatures of bismuth telluride sintered in box, microwave, and tube furnace at 300oC and 350oC.

Figure S12. The variation of the dielectric permittivity storage with frequency of bismuth telluride sintered in box, microwave, and tube furnace at 300oC and 350oC.

Figure S13. The variation of the dielectric permittivity loss with frequency of bismuth telluride sintered in box, microwave, and tube furnace at 300oC and 350oC.