Biodegradable Polysaccharide Grafted Polyacrylamide Inhibitor for Corrosion in CO2- Saturated Saline Solution

Supplementary Information

## 2.2 Microwave-Assisted Synthesis of Agar-Grafted-Polyacrylamide (AGGPAM)

Figure S1. Proposed reaction mechanisms for PAM graft polymerization onto agar chain.

## Contact Angle Measurements

Figure S2. Contact angle measurements of C-steel in (a) blank CO2-saturated 3.5 wt% NaCl with (b) 500 mg.L-1 AGGPAM inhibitor after 6 hours immersion at 25 °C.

| - Polished C-steel |  |  |  |
| --- | --- | --- | --- |
| - C-steel in blank |  |  |  |
| - C-steel in solution with 500 mg.L-1 AGGPAM |  |  |  |
| - AGGPAM Coated C-steel |  |  |  |

Figure S3. SEM micrographs of (a) polished C-steel samples in (b) blank CO2-saturated 3.5 wt% NaCl (c) with 500 mg.L-1 AGGPAM inhibitor immersed for 6 hours, and (d) AGGPAM coated steel sample before and after 6 hours immersion, all at 25 °C