Supporting information

Chitosan/Lignosulfonate Nanospheres as “Green” Biocide for Controlling the Microbiologically Influenced Corrosion of Carbon Steel

Pathath Abdul Rasheed 1, Ravi P. Pandey 1, Khadeeja A. Jabbar 1, Ayman Samara 1, Aboubakr M. Abdullah 2 and Khaled A. Mahmoud 1,3,*

1	Qatar Environment and Energy Research Institute (QEERI), Hamad Bin Khalifa University (HBKU), Qatar Foundation, Doha, P.O. Box 34110, Qatar; pabdul.rasheed@gmail.com (P.A.R.); rpandey@hbku.edu.qa (R.P.P.); KAbdulJabbar@hbku.edu.qa (K.A.J.); asamara@hbku.edu.qa (A.S.)

2	Center for Advanced Materials, Qatar University, Doha, P.O. Box 2713, Qatar; bakr@qu.edu.qa

3	Department of Physics & Mathematical Engineering, Faculty of Engineering, Port Said University, 42523 Port Said, Egypt

*	Correspondence: kmahmoud@hbku.edu.qa, Tel.: +974-4454-1694

Figure S1. The Nyquist plot of the coupon incubated in the abiotic media (A). The corresponding Bode plots are given in (B) and (C).

Figure S2. (A) The Nyquist plot of the coupon incubated with SRB with CS/LS with different concentrations from 0 to 1000 µg·mL−1. The impedance analysis was performed after 10 days of incubation. (B) The Rct vs concentration of CS/LS after 10 days of incubation. The error bar indicates the standard deviation from the three independent measurements.

Figure S3. The Nyquist plot of the coupon after 7 days of incubation in presence of CS/LS.

Figure S4. Nyquist plot of the incubated coupon after 15 days in SRB enriched media with 5% GA. Inset shows the fitting equivalent circuit. The inset shows the photographs of the incubation mixture of SRB + 5%GA after 15 days of incubation. For comparison, the photograph of  incubation mixture of  SRB + CS/LS is also given.

Figure S5. SEM images of the biofilm grown on the coupon surface after being incubated with SRB enriched media for 4 days without inhibitor (A) and in presence of 500 µg·mL−1 CS/LS (B).

Figure S6. EDS analysis of biofilm incubated in SRB enriched media without CS/LS (A) and with 500 µg·mL−1 CS/LS (B) after 35 days of incubation.

| Sample | Elements | Line | Mass (%) | 3 sigma | Atomic (%) | Intensity (cps/mA) |
| --- | --- | --- | --- | --- | --- | --- |
| Without CS/LS | 16 S | K | 12.42 | 0.13 | 10.22 | 6933.66 |
|  | 26 Fe | K | 44.31 | 0.32 | 20.93 | 217664.55 |
|  | O |  | 40.34 | 0.37 | 66.49 |  |
| With 500 µg.mL-1 CS/LS | 16 S | K | 9.59 | 0.10 | 7.27 | 4070.38 |
|  | 26 Fe | K | 22.02 | 0.13 | 9.59 | 74877.14 |
|  | O |  | 43.57 | 0.29 | 66.21 |  |

Figure S7. XRF analysis of the biofilm incubated in SRB enriched media without CS/LS and with 500 µg·mL−1 CS/LS after 35 days of incubation.

Figure S8. Profilometry of the bare carbon steel coupon surface. (A) 2D and (B) 3D images.

Figure S9. Profilometry images (2D and 3D) of the cleaned carbon steel coupon surface after 35 days of incubation in SRB without CS/LS (A and B) and SRB with 500 µg·mL−1 CS/LS (C and D) respectively.

Table S1. Composition of simulated seawater.

| Chemical Ion | Concentration (mg/L) | Part of Salinity (%) |
| --- | --- | --- |
| Chloride Cl- | 19345 | 55.03 |
| Sodium Na+ | 10752 | 30.59 |
| Sulfate SO4−2 | 2701 | 7.68 |
| Magnesium Mg+2 | 1295 | 3.68 |
| Calcium Ca+2 | 416 | 1.18 |
| Potassium K+1 | 390 | 1.11 |
| Bicarbonate HCO3−1 | 145 | 0.41 |
| Bromide Br− | 66 | 0.19 |
| Borate BO3− | 27 | 0.08 |
| Strontium Sr+2 | 13 | 0.04 |
| Fluoride F− | 1 | 0.003 |

Table 2. EIS fitting data.

| Coupon incubated in | Incubation time (day) | Rs (Ω·cm2) | Rf (Ω·cm2) | Rct (Ω·cm2) | Yf (mS·Secn/cm2) | nf | Ydl (mS·Secn/cm2) | nct | Cdl (μF·cm−2) | Cf (μF·cm−2) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SRB alone | 7 | 16.89 | 79.71 | 363.6 | 0.0143 | 0.65 | 0.0885 | 0.61 | 21335.44 | 20013.93 |
|  | 10 | 14.75 | 75.67 | 256.1 | 0.0526 | 0.99 | 0.0399 | 0.73 | 9290.29 | 21143.24 |
|  | 15 | 16.88 | 69.4 | 173.8 | 0.0116 | 0.99 | 0.0251 | 0.94 | 9801.80 | 13052.12 |
|  | 21 | 17.55 | 45.4 | 137.2 | 0.0475 | 0.89 | 0.0474 | 0.86 | 14401.77 | 32100.10 |
|  | 28 | 18.85 | 38.64 | 107.9 | 0.0274 | 0.99 | 0.0393 | 0.89 | 16228.08 | 26521.42 |
|  | 35 | 17.32 | 23.61 | 88.4 | 0.0060 | 0.99 | 0.0297 | 0.71 | 20674.88 | 6406.06 |
| SRB with CS/LS nanospheres | 7 | 20.99 | 292.7 | 609 | 0.00576 | 0.78 | 0.00658 | 0.95 | 2718.34 | 5155.09 |
|  | 10 | 21.61 | 249.2 | 468 | 0.01529 | 0.76 | 0.01779 | 0.89 | 4367.55 | 7611.33 |
|  | 15 | 23.95 | 209 | 312.8 | 0.00421 | 0.94 | 0.0270 | 0.88 | 6595.25 | 4824.20 |
|  | 21 | 25.71 | 129.7 | 254.6 | 0.011 | 0.83 | 0.0172 | 0.76 | 7687.26 | 10479.19 |
|  | 28 | 26.8 | 90.65 | 193.2 | 0.0706 | 0.99 | 0.0689 | 0.82 | 12131.15 | 19924.68 |
|  | 35 | 25.3 | 71.2 | 157.3 | 0.0621 | 0.99 | 0.0313 | 0.85 | 11880.12 | 23111.96 |